A heavy contract carpet sheet or tile with a great heritage. This durable fine ribbed product has become the benchmark for needle punched polypropylene carpet in education and public buildings sectors, and delivers a practical and hard wearing floor solution.

Rawson Carpet Solutions have been supplying Eurocord carpet in sheet and tiles to the education sector for over 50 years.

**Product Description:**Tile

**Fibre Type:** 80% Polypropylene 20% Polyester

**Fibre Weight:** 930g/m2

**Total Carpet Weight (+ 10%):** 4150g/m2

**Total Thickness (+ 10%):** 6.7mm

**Tile Dimensions (+ 10%):** 50cm x 50cm

**Backing Material:** Bitumen

**Tiles Per Box:** 20

**Product Description:** Sheet

**Fibre Type:** 80% Polypropylene 20% Polyester

**Fibre Weight (+ 10%):** 930g/m2

**Total Carpet Weight (+ 10%):** 1150g/m2

**Total Thickness (+ 10%):** 5.8mm

**Dimensions:** 2x30m